Fiber Burn Test

| Fiber | Fiber Type | Flame Reaction | Bead | After-Flame | Odor |
| --- | --- | --- | --- | --- | --- |
| Cotton | Cellulose Fiber | May flair when lit, burns | None | Continues to glow | Burning paper |
| Linen | Cellulose Fiber | May flair when lit, burns | None | Continues to glow | Burning paper |
| Rayon | Manufactured cellulose fiber | Burns without flame or melting | None unless there is a fabric finish | May glow longer than cotton | Burning paper |
| Silk | Protein Fiber | Burns slowly, curls away from flame | Dark bead easily crushed | Self-extinguishing | Burned hair or charred meat |
| Wool | Protein Fiber | Burns slowly, curls away from flame | Brittle dark, easily crushed | Self-extinguishing | Strong odor of hair or feathers |
| Acetate | Manufactured Fiber | Burns quickly, can flare even after flame is removed | Hard, brittle, uncrushable | Melts into a very hot bead, Drip Danger | Hot vinegar or burning pepper |
| Nylon | Manufactured Fiber | Quick burning due to fabric finish, shrinks to flame | Hard, grayish, uncrushable | Burns slowly and melts, self-extinguishing, Drip Danger | Celery |
| Polyester | Manufactured Fiber | Quick burning, shrinks away from flame, may flare | Hard dark round bead | Burns slowly, not always self-extinguishing | Slightly sweet, chemical |
| Acrylic | Manufactured Fiber | Flares at match-touch, shrinks away from flame, burns rapidly, hot sputtering flame, Drip Danger | Hard dark irregular shape | Continues to melt after flame is removed | Strong acrid fishy odor |