| TITLE: Manufactured Fibers Burn/Solubility/Microscope Observation 110 minute lab |
| --- |
| BEHAVIORAL OBJECTIVE: Students will be able to: Compare and contrast burning characteristics of manufactured fibers Discover and analyze the shapes of manufactured fibers under the microscope Determine the damaging solutions to manufactured fibers with a solubility test |
| STANDARD: Objective 20.0113-0301 Identify basic fibers, the characteristics, use and care of each textile. National Standards 16.2.1, 16.2.2, 16.2.5 |
| MOTIVATOR: Question of the day: “I am using a burn test to determine the fiber content on a textile. My results were as follows: it shrunk from the flame as it was placed near it, it burned in the flame, it extinguished itself when removed from the flame, it smelled like charred meat, and left a black irregular bead that crushed easily to a black powder. What is the probable fiber content? (silk or wool) Is further testing necessary to determine fiber content? (yes-microscope observation will tell the difference between silk and wool. Both fibers will dissolve in a sodium hypochlorite concentration) | SUPPLIES: None |
|  | TIME: 5 minutes |
|  | ACTIVITY #1 (TITLE AND DESCRIPTION: Lecture for the lab-“What is the purpose of this lab?” | TIME: 10 minutes |  |
| CONTENT: Standard test methods for fibers include qualitative and quantitative identification, as well as determination of physical features. When fiber content information is not available, it can usually be determined by a few simple tests. These tests-burning, microscopic observation, and solubility-are described on your lab sheets. Burning can identify the broad classes of cellulosic, protein, and thermoplastic fibers by ignition, odor, and residue. Microscopic observation and/or solubility in specific solvents can then usually distinguish fibers within each category. Testing methods and procedures are outlined by the AATCC and the ASTM organizations. We will be using both standards of testing throughout the semester. This is the same for both manufactured and natural fibers. There are additional properties of manufactured fibers. When hot and melted, if you touch the end of the pick to the fiber you should be able to pull away and leave a thread (like melted cheese strings from pizza). They are also thermoplastic fibers. If you heat them, patterns will be set permanently until the next time they are heated. | SUPPLIES: Lab report worksheets (see the end of the lesson) Aprons under sink in FL 310 Gloves under sink in FL 310 Beakers in cabinet under desk Take Supplies to ASTE 106 |
| PROCESS QUESTIONS: What are some advantages to a manufactured fiber over a natural fiber? (convenience, cost, thermal plasticity, renewable resource, etc) What is the AATCC? (American Association of Textile Chemists and Colorists.) What is the ASTM? (American Society for Testing and Materials.) Why perform all the tests on textiles? (Quality, identification, characteristics, end uses, etc.) |
|  | ACTIVITY #2 (TITLE AND DESCRIPTION: Burn testing | TIME: 25 minutes |  |
| CONTENT: AATCC test method 20-2002 (AATCC technical manual page 41) Students will take samples of manufactured fiber fabrics and burn small pieces of fiber to determine the characteristics of the fibers when being burned. They will write their findings on their lab report. Students will look at: The flame-whether the fabric approaches the flame or is resistant to the flame. Does it burn itself out or continue to feed the flame. The smoke-what color (i.e. black, grey, white); The smoke-what smell (i.e. burning hair, grass, chemicals); The ash-what color and consistency (i.e. soft bead, ash, hard, black, grey); Threading of the fiber-yes or no | SUPPLIES: Matches Tea light candles Candle holders Metal picks Tweezers Tin foil Fabric swatches of: polyester acetate nylon rayon acrylic olefin |
| PROCESS QUESTIONS: Did any of the fibers tested thread out? (Yes-except rayon or lyocell.) Why did some of the fibers not thread out? (because they are manufactured with cellulosic fibers which do not have threading capability) |
|  | ACTIVITY #3 (TITLE AND DESCRIPTION: Solubility testing | TIME: 25 minutes |  |
| CONTENT: AATCC test method 20-2002 (AATCC technical manual page 42) Students will take samples of the manufactured fibers and place a ½ inch square piece in a beaker and cover the test sample with solution and stir. After 3 minutes, they will see if there is any reaction to the fabric. After 10 minutes they will observe again. Reactions may include: Soluble (dissolves) Insoluble (no change) Forms plastic mass Students will test 3 samples of their choice in 3 solutions. | SUPPLIES: Beakers Stir sticks Acetone Bleach (Sodium Hypochlorite) Vinegar (acetic acid) Salicylic Acid (beta hydroxy acid derived from the bark of the willow tree) Sulfuric Acid Samples of : polyester acetate nylon rayon acrylic olefin |
| PROCESS QUESTIONS: 1. What reactions surprised you? (answers will vary) |
|  | ACTIVITY #4 (TITLE AND DESCRIPTION: Microscope Observation | TIME: 25 minutes |  |
| CONTENT: AATCC test method 20-2002 (AATCC technical manual pages 44-54) Students will observe samples that have pre-plated with distilled water and numbered 1-8 by the instructor. They will look at the slides under the microscope. On their lab report, there will be space for them to draw the longitudinal view of the fiber under 500 x magnification. | SUPPLIES: Raw fiber samples of: polyester acrylic nylon rayon acetate olefin modacrylic vinyl Microscopes Slides Distilled water Copies of illustrations from AATCC technical manual (p. 44-54) |
| PROCESS QUESTIONS: Do any of the fibers look the same? (no, it may be difficult to tell) Which fiber had the oddest shape? (answers will vary) |
|  | ACTIVITY #5 (TITLE AND DESCRIPTION: Correcting Lab Reports | TIME: 10 minutes |  |
| CONTENT: Students may use the table in their book to self correct their lab reports. | SUPPLIES: Fabric Science textbook Tables on pages 28, 30 Copies of tables for students |
| PROCESS QUESTIONS: |
|  | ACTIVITY #6 (TITLE AND DESCRIPTION: Catch Up | TIME: |  |
| CONTENT: Students may use the time to finish any lab work from the week before. | SUPPLIES: |
| SUMMARY: Students will be able to generally identify manufactured fibers using 3 simple tests-burning, solubility, and microscope observation. |
| STUDENT EVALUATION; Lab reports will be due at the beginning of class next week February 5th by 3:30 p.m. They will be evaluated for completeness and accuracy. They will be worth 50 points and 20 attendance points. Points will be distributed as follows: 36 burn test table answers (each space answered) @ .66 points each 21 solubility answers @ .66 points each 18 microscope answers (sketch and label) @ .66 points each Answer key (or diagrams and answer tables) follow lesson plan |
| TEACHER EVALUATION: Did the students accomplish the behavioral objectives? Did the transitions between activities go smoothly? What needs to be re-evaluated before teaching it next time? |
| OPTIONAL ACTIVITY: Students may test samples out of their swatch kit to predict the characteristics of each of the tests. Reactions may vary due to blends of fibers, finishes, and dyes. |
| REFERENCES: AATCC technical manual. (A. B. Chehna, Ed.) (2004, Vol. 79). Research Triangle Park, NC: American Association of Textile Chemists and Colorists. Collier, B. J., & Epps, H. H. (1999). Textile testing and analysis. Upper Saddle River, New Jersey: Merrill. Price, & Cohen. Fabric science swatch kit. http://www.sciencestuff.com/ Chemical solutions available for purchase. All solutions listed in Fabric science 8th edition p. 30, (table 2.3). |

Lab #4 Lab Report Manufactured Fibers

Burn/Solubility/Microscope Observation

- Burn Test

Procedure

    - Take a small piece of fabric sample (1/2 inch square, held in tweezers) and place close to the side of a small flame.  Note if the fibers melt, shrink from the flame, or rush towards the flame.

    - Move the fibers into the flame.  Note whether the fibers will burn when held in the flame.  Remove from the flame very slowly and carefully.  Note whether the fibers continue to burn outside of the flame or smolder.  Make sure that the fiber was ignited before making this latter observation.

    - Blow out the flame, if still burning, and smell the smoke.  Note the odor and examine the color and nature of any ash residue.

    - At the end of class, you may compare your answers to the observed behaviors of the fibers to the expected behaviors listed in your textbook.

| Name of Fiber | Characteristics or Behaviors of the Fiber and the Flame |
| --- | --- |
|  | Does it melt, shrink, or rush towards the flame from the flame as it approaches? | Does the fiber burn quickly, slowly or smolder in the flame? | Does the fiber continue to burn after being removed from the flame or does it self-extinguish? | What does the ash look like? (Color, texture, etc.) | What does the smoke look like? (Color, appearance, etc.) | What does the smoke smell like? |
| Polyester |  |  |  |  |  |  |
| Acrylic |  |  |  |  |  |  |
| Nylon |  |  |  |  |  |  |
| Rayon |  |  |  |  |  |  |
| Acetate |  |  |  |  |  |  |
| Olefin |  |  |  |  |  |  |

Additional Notes/Questions:

- Solubility Test

Procedure

- Work in groups of 3.  Each student will be responsible for recording the results on their own lab sheets.

- Choose 3 fabrics to test and 3 solvents to test with.

- At room temperature (20۫C°) place a small sample (1/2” square) of the fibers or fabric swatch in a beaker and barely cover with the test solvent.  Let fiber sit in the solution for 3 minutes.

- Note if the fiber dissolves completely, softens to a plastic mass or remains insoluble.

- Return to test samples and re-observe after 10 minutes.  Observes any changes.

- At the end of class, you may compare your answers to the observed behaviors of the fibers to the expected behaviors listed in your textbook.

| Name of Fiber | Characteristics or Behaviors of the Fiber and the Solution |
| --- | --- |
|  | Name of Solvents |
| 1. | 3 min |  |  |  |
|  | 10 min |  |  |  |
| 2. | 3 min |  |  |  |
|  | 10 min |  |  |  |
| 3. | 3 min |  |  |  |
|  | 10 min |  |  |  |

Additional Notes/Questions:

- Microscope Observation

Procedure

  - Place the fibers plated in microscope slides into the microscopes and focus to 500x magnification.

  - Observe the fiber characteristics as seen in traverse sections and draw your observations in the circles provide.

  - Compare your drawn observations with the pictures provided in your textbook and in the AATCC  Vol 79, 2004 reference book (pages 44-54) and label the appropriate samples.

Answer Key

Burn Chart

Solubility Answer Chart

| Name of Fiber | Acetic Acid (vinegar) | Salicylic Acid (facial cleanser) | Sulfuric Acid (toilet cleaner) | Acetone (fingernail polish remover) | Hydrochloric acid (chlorine bleach) |
| --- | --- | --- | --- | --- | --- |
| cotton | Nothing | Nothing | Soluble | Nothing | Nothing |
| flax | Nothing | Nothing | Soluble | Nothing | Nothing |
| jute | Nothing | Nothing | Soluble | Nothing | Nothing |
| silk | Nothing | Nothing | Soluble | Nothing | Soluble |
| wool | Nothing | Nothing | Nothing | Nothing | Soluble |
| children’s sleepwear | Depends on fiber content of sleepwear-cotton would be soluble in sulfuric acid, wool and silk will be soluble in sodium hypochlorite, vinyon and acetate would be soluble in acetone, and acetate is soluble is acetic acid |

Microscope Answer chart

Diagram is subjective grading-does it look like a diagram of a fiber?

Labeling

- polyester

- rayon

- olefin

- nylon

- acrylic

- modacrylic

- acetate

- vinyon